| DAFA - DAM | DATA SHEET DATE : 09/01 |  |
| --- | --- | --- |
| PRODUCT NAME : CLARCEL DIC/B This product is manufactured under ISO 9002 (N°.1993/1554a) certification. |  |  |
| ________________________________________________________________________________ |  |  |
| PRODUCT NATURE AND COMPOSITION : CLARCEL DIC/B filter aid is obtained by the means of calcination / activation of purified diatomite, with a fusible alkali. The CLARCEL DIC/B is white in colour.. ________________________________________________________________________________ |  |  |
| APPLICATIONS AREAS : CLARCEL DIC/B is aimed at separation of solids from liquids through first precoat, as a mecanical protection of filtration septum. - Clarification of beverages : Beer, Fruit juice, Cider, Wine, ... - Clarification of chemical and pharmaceutical products |  |  |
| SPECIFICATIONS : (1) METHODS (3) CONTROLS UNITS VALUES 140 1301 Permeability DARCY 0,88 - 1.62 140 1302 Cake Density g/cm3 £ 0,430 140 1303 Retained on 50 µm % in weight £ 15 |  |  |
| AVERAGE CHARACTERISTICS : (2) METHODS (3) CONTROLS UNITS VALUES 140 1304 Retained on 500 µm % in weight 0,1 140 1311 Moisture % 0,5 140 1312 Loss on ignition % 0,5 ________________________________________________________________________________ |  |  |
| PACKING : 25 kg net paper bags Paletts or 525 kg or 900 kg CLARCEL can be stored over a 2 years period, from delivery date, if maintained in its original packing, in a dry warehouse, free of volatile matter. ________________________________________________________________________________ |  |  |
| (1) The specifications are guarenteed for each lot. |  |  |
| (2) The given values are indicative. |  |  |
| (3) CECA method. |  |  |
| SAFETY DATA SHEETS AVAILABLE UPON REQUEST. |  |  |

| DAFA - DAM |  |  |  | ANALYSES TYPES PRODUIT FINI CLARCEL DIC/B |  |  |  |  |  |  | ISSUE : 2 DATE : 03/01 |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Particle Size Distribution Curve for CLARCEL DIC/B This analysis represents the average annual sample for 1996 |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Particle size distribution (% of volume) |  |  |  |  |  |  | Typical Chemical Analysis |  |  |  |  |  |  |  |
|  |  | > 1 µ | 97.3 |  | % |  |  |  | SiO2 | 88 |  | % |  |  |  |
|  |  | > 5 µ | 89.9 |  | % |  |  |  | Al2O3 | 2.9 |  | % |  |  |  |
|  |  | > 10 µ | 79.9 |  | % |  |  |  | Fe2O3 | 2.3 |  | % |  |  |  |
|  |  | > 20 µ | 56.4 |  | % |  |  |  | TiO2 | 0.12 |  | % |  |  |  |
|  |  | > 35 µ | 33.3 |  | % |  |  |  | CaO | 0.9 |  | % |  |  |  |
|  |  | > 50 µ | 22.4 |  | % |  |  |  | MgO | 0.3 |  | % |  |  |  |
|  |  | > 75 µ | 11.3 |  | % |  |  |  | K2O | 0.22 |  | % |  |  |  |
|  |  | > 100 µ | 6.6 |  | % |  |  |  | Na2O | 3 |  | % |  |  |  |
|  |  | > 200 µ | 1.7 |  | % |  |  |  |  |  |  |  |  |  |  |
|  |  | > 350 µ | 0.4 |  | % |  |  |  |  |  |  |  |  |  |  |
|  |  | > 500 µ | 0 |  | % |  |  |  |  |  |  |  |  |  |  |

The above given information represent typical values.

Under no circumstances should they be regarded as SPECIFICATIONS